ŠÍŘENÍ INDENTAČNÍCH TRHLIN V KERAMICKÝCH LAMINÁTECH S PEVNĚ VÁZANÝMI VRSTVAMI

Iing. Hynek Hadraba, Ph.D., Ústav fyziky materiálů AV ČR, v.v.i., Žižkova 22, 616 62 Brno, Česká republika, hadraba@ipm.cz

Ing. Zdeněk Chlup, Ph.D., Ústav fyziky materiálů AV ČR, v.v.i., Žižkova 22, 616 62 Brno, Česká republika

doc, RNDr. Karel Maca, Dr., Vysoké učení technické v Brně, Technická 2896/2, 616 69  Brno, Česká republika

Dipl.-Ing. Dr. Raúl Bermejo, MontanUniversität Leoben, Peter Tunner-Straße 5, A-8700  Leoben, Rakousko

Key words: electrophoretic deposition, slip casting, ceramic laminates, crack propagation

Crack propagation in ceramics laminates with strongly bonded interfaces

Crack propagation through layered composites based on Al2O3 and ZrO2 was studied. The strongly bonded laminates with single-component layers and laminates with two-component layers were prepared via electrophoretic deposition and slip casting respectively. Laminates of different pre-defined thicknesses and composition contained different magnitudes of residual stress. Cracks, produced by an indentation technique, propagated towards layer interfaces deflected towards the interface in the compressed layers and away from the interface in the layers containing tension stress. Changes in the direction of crack propagation were described for the whole range of angles of incidence (0° - 90°). The biggest change in the crack propagation was observed, irrespective of the magnitude of residual stress in the layers.

Acknowledgement: This work was carried out under support of Czech Science Foundation projects GACR 106/05/0495 and GACR 106/06/0724.