THE EFFECT OF MECHANICAL ALLOYING ON INDENTATION PROPERTIES OF MoSi2-SiC SYSTEM

prof. ing. Ladislav Pešek, CSc., Department of Materials Science, Faculty of Metallurgy, Technical University of Košice, Letná 9, 042 00 Košice, Slovakia, ladislav.pesek@tuke.sk

ing. Zuzana Vadasová, Department of Materials Science, Faculty of Metallurgy, Technical University of Košice, Letná 9, 042 00 Košice, Slovakia

ing. Pavol Zubko, Department of Materials Science, Faculty of Metallurgy, Technical University of Košice, Letná 9, 042 00 Košice, Slovakia

ing. Beáta Ballóková, Ústav materiálového výskumu SAV, Watsonova 47, Košice, 04353, Slovensko

prof. ing. Michal Besterci, DrCs., Institute of Materials Research, Slovak Academy of Sciences, Watsonova 47, 043 53 Košice, Slovakia

doc. ing. Olga Bláhová, Ph.D., New Technologies Research Centre, University of West Bohemia, Univerzitní 8, 306 14  Plzeň, Czech Republic

Key words: DSI, instrumented indentation hardness testing, indentation hardness, indentation modulus, mechanical alloying

Using the depth sensing indentation technique (DSI): (i) the data of indentation modulus EIT and indentation hardness HIT; (ii) effect of the introduced vol.% of SiC particles on both EIT and HIT value; (iii) homogeneity of properties, were experimentally investigated on MoSi2-SiC mechanically alloyed system, taking the testing conditions into consideration. SiC particles in amount of 0; 5; 10 and 15 vol.% were introduced into the MoSi2 matrix.

Conclusion: The measured data EIT = 320 – 420 GPa and HIT = 12 – 23 GPa depend on both vol.% of particles and indentation force used. With increasing vol.% of particles increase both EIT and HIT; however, the significant influence was observed in the range of 0 – 10 vol.%. The increase of HIT data is more expressive (30 – 100 %) than that of EIT data (approx. 20%). The indentation size effect (ISE) affects both EIT and HIT data for the indentation loads up to 300 mN.

Aknowledgement: This work was supported by the VEGA Grant No. 1/3210/06 and partly by the SK-CZ project SK-132/CZ-109.

VPLYV  MECHANICKÉHO  LEGOVANIA NA INDENTAČNÉ VLASTNOSTI SYSTÉMU MoSi2-SiC

prof. ing. Ladislav Pešek, CSc., Katedra náuky o materiáloch, Hutnícka fakulta, Technická univerzita v Košiciach, Letná 9, Košice, 04200, Slovensko, ladislav.pesek@tuke.sk

ing. Zuzana Vadasová, Katedra náuky o materiáloch, Hutnícka fakulta, Technická univerzita v Košiciach, Letná 9, Košice, 04200, Slovensko,

ing. Pavol Zubko, Katedra náuky o materiáloch, Hutnícka fakulta, Technická univerzita v Košiciach, Letná 9, Košice, 04200, Slovensko,

ing. Beáta Ballóková, Ústav materiálového výskumu SAV, Watsonova 47, Košice, 04353, Slovensko

prof. ing. Michal Besterci, DrCs., Ústav materiálového výskumu SAV, Watsonova 47, Košice, 04353, Slovensko

doc. ing. Olga Bláhová, Ph.D., Nové Technologie Výzkumné Centrum, Západočeská univerzita v Plzni, Univerzitní 8, Plzeň, 60314, Česká Republika

Klíčová slova: DSI, inštrumentovaná skúška tvrdosti, indentačná tvrdosť, indentačný modul pružnosti,  mechanické legovanie

Metódou inštrumentovanej tvrdosti (DSI – depth sensing indentation) boli u kompozitu MoSi2-SiC experimentálne stanovené: (i) indentačný modul pružnosti EIT a indentačná tvrdosť HIT; (ii) vplyv objemu pridávaných častíc SiC na EIT a HIT; (iii) homogenita vlastností; v závislosti od podmienok skúšky. Bol analyzovaný kompozit s 0; 5; 10; 15% objemového podielu častíc SiC. Bolo zistené, že:

Hodnoty jednotlivých vlastností sú: EIT = 320 – 420 GPa; HIT = 12 – 23 GPa v závislosti od obj. % častíc a od použitej indentačnej sily. Vplyv dopovania časticami je významný v rozsahu 0 -10 % obj., s rastúcim objemom pridávaných častíc SiC rastú aj hodnoty EIT a HIT. Nárast HIT je výraznejší (30 – 100 %) ako nárast EIT (cca 20%). ISE (indentation size effect) funguje pre EIT aj pre HIT v rozsahu 0 – 300 mN zaťažujúcej indentačnej sily.

Poďakovanie: Publikácia vznikla pri riešení projektu VEGA No. 1/3210/06 a pri riešení SK-CZ projektu SK-132/CZ-109.